Speeds and Feeds for 5400 series coolant fed drills. Solid carbide coolant thru drill with 140 deg split point, Tialn coated. Drills are either made in USA or Germany.

Hardness                                       Feed Per Rev.

Material                                     Bhn       SFM   5/32”dia   ¼”      3/8”    ½”      ¾”     1”

| Aluminum 2011,2024,6061,7075 | -- | 500 | .0045 | .0065 | .0075 | .0085 | .01 | .012 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Free Machining 12L14, 1215,11L17 | 80-150 | 350 | .004 | .0055 | .007 | .008 | .0095 | .0011 |
| Low Carbon Steel 1008, 1018, 1020 | 125-175 | 290 | .0035 | .0047 | .0055 | .0065 | .0075 | .009 |
| Medium Carbon Steel 4140, 8620 | 200-280 | 250 | .003 | .0045 | .0055 | .0065 | .0075 | .009 |
| Tool Steel, H.S.S A2,D2,M2,M42 | 300-400 | 120 | .0025 | .0035 | .004 | .0045 | .0058 | .007 |
| Cast Iron | 120-175 | 300 | .0045 | .0055 | .007 | .008 | .0095 | .011 |
| Stainless Steel 300 Series | 160-200 | 180 | .003 | .004 | .0055 | .0065 | .0075 | .009 |
| Stainless Steel 400 Series | 180-260 | 150 | .003 | .004 | .0055 | .0065 | .0075 | .009 |
| Stainless Steel 15-5, 17-4 | 160-200 | 150 | .003 | .004 | .0055 | .0065 | .0075 | .009 |
| Titanium 6AL-4V | 320-280 | 50 | .003 | .0035 | .005 | .006 | .007 | .0075 |
| Inconel 625, 718 | 280-320 | 50 | .0028 | .003 | .0045 | .005 | .005 | .006 |
| Copper, Bronze | 120-160 | 300 | .004 | .005 | .006 | .007 | .009 | .01 |
| Brass (360 half hard) | -- | 500 | .0045 | .0065 | .008 | .0085 | .01 | .012 |

Coolant pressure suggestions             450psi 320      260      150     100    80psi

Feed Per Rev. is based on standard cutting conditions

Feedrates can be increased up to 30% if cutting conditions are favorable. Please use our    ER series coolant sealing collets with these drills for perfect coolant sealing and proper coolant flow to the drill.

6 guidelines for best cutting results

| keep tip runout less than .001 | Make sure drill is perpendicular | Use coolant sealing collets |
| --- | --- | --- |
| workpiece rigidity is important | Use quality tool holder and collet | Provide highest coolant pressure |

Note: Cutting speeds, feeds, and lubrication data are given as starting values only. Parameters should be varied to suite your particular conditions. MariTool is constantly improving products, tolerances, and reliability. As such, these speeds and feeds are subject to change without prior notice. Cutting tools may shatter and or produce dangerous fumes when being used. Appropriate protection is advised.                                                                                                                                           Rev A