Speeds and Feeds for Series 2500 Double Angle Chamfer Milling Cutters.

High Speed Steel

2500 Double Angle Chamfer Milling Cutters are Made in the USA.

| Material | Hardness Bhn | SFM |
| --- | --- | --- |
| Aluminum 2011,2024,6061,7075 | * | 350 |
| Free Machining 12L14, 1215,11L17 | 80-150 | 80 |
| Low Carbon Steel 1008, 1018, 1020 | 125-175 | 60 |
| Medium Carbon Steel 4140, 8620 | 200-280 | 50 |
| Tool Steel, H.S.S A2,D2,M2,M42 | 300-400 | 45 |
| Cast Iron | 120-175 | 75 |
| Stainless Steel 300 Series | 160-200 | 55 |
| Stainless Steel 400 Series | 180-260 | 40 |
| Stainless Steel 15-5, 17-4 | 160-200 | 40 |
| Titanium 6AL-4V | 320-380 | 20 |
| Inconel 625, 718 | 280-320 | 20 |
| Copper, Bronze | 120-160 | 200 |
| Brass (360 half hard) | * | 380 |

General starting point for feed per tooth is .001-.005 inches.  Smaller diameter cutters should be on the lower range while larger diameter cutters can be feed on the higher range. Reduce FPT and SFM with deep slots and or long overhangs. Flood coolant is always helpful and helps clear the chips from the teeth.

6 Guidelines for Best Cutting Results

| keep overall gage length short | keep tool concentricity low | climb milling is generally best |
| --- | --- | --- |
| workpiece rigidity is important | avoid double cutting chips | Use plenty of coolant |

Note: Cutting speeds, feeds, and lubrication data are given as starting values only. Parameters should be varied to suite your particular conditions. MariTool is constantly improving products, tolerances, and reliability. As such, these speeds and feeds are subject to change without prior notice. Cutting tools may shatter and or produce dangerous fumes when being used. Appropriate protection is advised.